Product information

SUNOCO

Vacuum Pump Oil

Description	Special oil for the lubrication of high vacuum pumps.

Application 	Recommended for use in the majority of high vacuum pumps working with an absolute pressure of 50 microns of mercury (or 0,05 torr) or even lower.

Properties 	- Exact viscosity for fast and uniform oil distribution and perfect sealing of

the narrow passages between  pump blades, rotor and cylinder walls.

- Very low vapour pressure. Good film strength for minimum friction and

lowest possible wear.

- Suitable water separating properties. High oxidation stability for extended

oil life time. Relatively low water content.

- Specially adapted for vacuum type applications in the refrigeration

industry.

Typical analysis  :

| Density at 15°C | 0.881 |
| --- | --- |
| Viscosity at 40°C / cSt | 68 |
| Viscosity at 100°C / cSt | 8.7 |
| Viscosity index | 98 |
| Flash point °C | 230 |
| Pour point °C | -30 |
| TAN mg KOH/g | 1.0 |
| Colour | L1.5 |